Liquid Indium real and virtual experiment
Liquid Indium:
Very low scattering cross section
Very high absorption
Never measured with neutrons
Proposal includes both real and virtual experiment:
Simulation showed we would be able to measure the quasi-elastic line
Around the first structure peak in S(q).
Experiment:
Levitation furnace (gas flow+laser)
T=450 K
IN22 Ei=30.8 meV
Team: E. Farhi, P. Willendrup, L.P.Regnault, McStas <mcstas.org>

---
Liquid Indium real experiment
Data includes contribution from the furnace and the B4C nozzle.
Sample is a f=4mm diameter sphere
Experiment produces...
?
Background ?
Structure peak position

---
Liquid Indium: Ab-Initio Molecular Dynamics
We use VASP
200 atoms in a 17 Å cube
Record atoms dynamics for 36 ps
Compute S(q,w) using nMoldyn
Coherent part
Incoherent part
We show here the measurement range
Compared to experiment,
computed S(q,w) is very clean

---
Liquid Indium: Virtual experiment
We use McStas <mcstas.org> to model the reactor, the H25 supermirror
Guide and the IN22 triple-axis spectrometer.
Model includes levitation furnace and nozzle.
We run on 80 cores for 4 hours to
simulate all q-energy scans.

---
Liquid Indium: Virtual experiment (cont'd)
Total signal shows
a tail after the
structure peak
Coherent part
Incoherent part
Furnace contribution
Virtual experiment enables to
prepare and understand
the measurement.
l-In measured with neutron